## Slide 1
2023.5.23 @ IOP, CAS
于伟强
中国人民大学物理学系
量子磁性材料中量子相变与临界现象的核磁共振研究

## Slide 2
OUTLINE
0. Introduction to quantum critical point (QCP）and NMR
I. KT phase in a 2D TLAFM.
Ref： NC 11, 5631 (2020)
II. Quantum criticality and emergent E8 state in Quasi-1D Ising magnet under transverse field.
Ref: PRL 123, 067203 (2019); PRL 127, 077210 (2021)
III. Filed induced proximate Kitaev QSL in a honeycomb compound -RuCl3.
Ref: PRL 119, 227208 (2017)
IV. NMR evidence of a proximate DQCP in SrCu2(BO3)2 .
Ref: arXiv:2204.08133 (to appear in Science)

## Slide 3
Collaborators
Renmin University of China
Yi Cui, Cong Li, Xuefei Liu, Ze Hu
Huihang Lin, Ning Xi, Rong Yu
Boston University
Kai-Hsin Wu, Anders W. Sandvik
Beijing Institute of Technology
Lu Liu
Institute of Physics, CAS
Wenshan Hong, Shiliang Li
…Also thanks to Wenan Guo, Bruce Normand…
Notes: Who provided extensive numerical simulations to understand our data… Who provide the very high quality single crystals

## Slide 4
I. Introduction to Quantum Critical Point
(QCP, 量子临界点)

## Slide 5
量子临界点：零温的有序-无序二级相变
Quantum Phase Transitions, by Sachdev
“经典”相变 (T>0)
量子相变 （ T = 0 ）
铁磁体二级相变
经典朗道相变理论
量子临界区域：非费米液体……
g: 压强、磁场、掺杂

## Slide 6
朗道相变理论：有序-有序（两种不同对称破缺态）之间为一级量子相变

## Slide 7
Magnetic driven Deconfined Quantum Critical Point (DQCP)：
产生自旋子解禁闭（分数化元激发）的新途径!
DQCP:违反朗道图像的二级量子相变？

## Slide 8
12 T + 1.5 K+ 2.4 GPa
16 T
2.4 GPa
25 mK
(bottom loading)
NMR+ 高压、强磁场、极低温 @ 人民大学
8 GPa (CAC)
10 T
(with IOP, JG Cheng)

## Slide 9
Condensed-matter NMR: A local, low-energy magnetic probe
B
NMR lineshape: static spin/charge distribution
A sensitive probe of electronic charge and magnetism, and their low-energy fluctuations.

## Slide 10
铁基超导
FeSe 条纹磁结构 PRL 2016
自旋单态配对 PRL2011
超导和反铁磁微观共存 PRL2012
超导和磁涨落 PRL 2013
(, ) 电荷序 PRB 2016
氢化超导和核磁共振
Sci Bull 2018

## Slide 11
Emergent U(1) symmetry and BKT phase transition in a triangular-lattice Ising Antiferromagnet

## Slide 12
2D XY model with U(1) symmetry:
No long-range order at finite temperature
Direct experimental evidence is lacking for XY magnets !!
BKT phase transition and vortex excitations

## Slide 13
TmMgGaO4
Tm
Mg, Ga
O
a=3.4195(4) Å
c=25.1231(13) Å
Interlayer = 8.3774Å
Tm3+ : 4f12
L=5 (l=2,3), S=1 ()
J=6
YbMgGaO4, Yuesheng Li et al.,
PRL 117, 097201 (2016)

## Slide 14
Non-Kramers doublets and intrinsic transverse field
Changle Liu et al., Phys. Rev. B 98, 045119 (2018)
Changle Liu et al., PRR 2,043013(2020)

## Slide 15
R. Moessner and S. L. Sondhi, PRB 63, 224401 (2001
King, AD et al., Nature 560, 456(2018)
Order by disorder and Emergent Z6 symmetry in transverse field of triangular lattice AFM

## Slide 16
Kosterlitz-Thouless melting of magnetic order
H. Li et al., Nat. Commun. 11, 1111(2020)

## Slide 17
Anisotropic spin model : gab~0
F. A. Cevallos et al., Mater. Res. Bull. 105, 154–158 (2018).

## Slide 18
NMR evidence of Magnetic ordering
NMR spectra
Knight shift
ordering temperature
TL ≃ 0.9 K

## Slide 19
plateau-like structure between
TU ≃ 1.9 K and TL ≃ 0.9 K
The hallmark of a BKT phase:
A fluctuating phase with diverging correlation length but no long-range order
Experimental evidence of BKT phase in TMGO

## Slide 20
Susceptibility scaling
QMC
Kedar Damle,
PRL 115, 127204 (2015)
Z. Hu et al.,
Nature Commun. 11, 5631 (202RL0)

## Slide 21
Phase diagram of TMGO under out-of-plane field
A BKT phase between TL and TU under zero out-of-plane field
A field induced quantum phase transition at the high-field side of the dome
Z. Hu et al., Nature Communications 11, 5631 (2020)

## Slide 22
ii. Emergent E8 algebra state in quasi-1D Ising antiferromagnet with transverse field

## Slide 23
A pedagogical model for Quantum Phase Transitions:
1D Ising-model in a transverse field
S. Sachdev, Quantum Phase Transitions (2011）
1D Phase diagram
deconfined spinons
Gapped ()
Gapped ()
Quasi-1D Phase Diagram
Renormalized classical
1D fluctuations
3D
3D quantum criticality
1D

## Slide 24
From the Ising chain to the XXZ chain at zero-field
Mikeska & Kolezhuk, in Quantum Magnetism (2004）
two-spinon continuum

## Slide 25
Y. Cui et al., PRL 123, 067203 (2019)
SrCo2V2O8
TcrL ∼ |H − HC2|
1D critical exponent νz = 1
H. Zou, Y. Cui et al., PRL 127, 077210 (2021)
BaCo2V2O8
E8 particles at a hidden 1D QCP
准一维横场依辛模型的自旋子束缚态—E8态

## Slide 26
Ising-chain Ferromagnet CoNb2O6 in a transverse field
W. Kinross et al., PRX 4, 031008 (2004)
3D Kink confinement at H = 0
E8 spectrum at H < ~ HC
R. Coldea at al., Science 327, 177 (2010)

## Slide 27
4.8o
Screw chain antiferromagnet BaCo2V2O8 & SrCo2V2O8
space group: I41cd a=b=12.267 Å c=8.424 Å
space group: I41/acd
a=b=12.444 Å c=8.4153 Å
Z. He et al. 2005 & 2006;Bera et al. 2017;
Q. Faure et al. 2018.....
BaCo2V2O8
SrCo2V2O8
4-site period Opposite screwing direction for n.n chains
J  3 mev,   2 J’  0.17 mev

## Slide 28
(Ba,Sr)Co2V2O8: Quasi-1D XXZ model with easy-axis anisotropy
BaCo2V2O8
J  2.87 mev,   1.89
J’  0.17 mev
SrCo2V2O8
J  3.7 mev,   2.1
Larger J, but lower TN
Kimura PRL 99, 087602 (2007)
Q. Faure et al., Nat. Phys. 14, 716 (2018)
….
Strong suppression of the AFM ordering by a longitudinal field
S = 1/2
Kimura 2013; Bera 2014; Wang 2015 …
H//c

## Slide 29
4-period staggered Hz
2-period transverse Hy : Strong suppression of AFM
H//[110]
H//[100]
Induced staggered fields in BaCo2V2O8 with H//[0 1 0]
H//[100]:
a 4-period staggered Hz
S. Kimura, et al., JPSJ 82, 033706 (2013)
H0 || a induces a staggered field H0 along the b-axis
Hy/H0=0.4 ; Hz/H0=0.14
H//[110]:

## Slide 30
BaCo2V2O8 with H || [010] :
A Topological quantum phase transition?
Q. Faure et al., Nat. Phys. 14, 716 (2018)
High-filed (Hc<H<Hs),
magnon-like excitations
Low-filed (H<Hc),
spinon excitations
H || b induces 2-site period Ha

## Slide 31
Z. Wang, et al., PRB 94, 125130 (2016)
THz study of SrCo2V2O8 with H || b : spinon confinement
Linear confining potential by the interchain couplings
From confined spinons to fermions

## Slide 32
Effective staggered field induced by periodic O-Co-O tilting in BaCo2V2O8 and SrCo2V2O8
A. K. Bera et al., RRB 96, 054423 (2017)
Y. Cui et al., PRL123, 067203 (2019)
Hy/H0=0.4
Hz/H0=0.14
Hy/H0=0.29
Hz/H0=0.14
Effective staggered field

## Slide 33
1D QCP identified by NMR measurements
TN: 3D order
1/T1 ∼ T −0.75e−Δ/KBT
Δ(H) ~ H −
 : 4.7 ±0.3 T
H. Zou et al., PRL 127, 077201 (2021).

## Slide 34
E8 excitation spectrum near the 1D QCP
T = 0.4 K
Red vertical lines:
8 single E8 particles
Quantum E8 integrable field theory
iTEBD
INS dynamical spectra agrees with analytical and numerical results
H. Zou et al., PRL 127, 077201 (2021).

## Slide 35
H = 4.7 T: the best agreement with the E8 predictions
H. Zou et al., PRL 127, 077201 (2021).
INS spectra peaks at different transverse field

## Slide 36
Phase diagram of BaCo2V2O8 in transverse field
H. Zou et al., PRL 127, 077201 (2021)
3D QCP at = 10.4±0.1 T
1D QCP at = 4.7±0.3 T
Realized full E8 spectrum at 1D QCP
Not a E8 symmetry!
Journal Club of CMP 推荐/ 每月1篇
By M. Oshikawa

## Slide 37
iii. Field-induced a gapless proximate Kitaev spin liquid in α-RuCl3

## Slide 38
A. Kitaev, Ann. Phys. 321, 2 (2006).
Exactly solvable
Pauli Matrix
under field:
Gapped excitations
Non-Abelian Anyons
2D Spin liquid: Kitaev model in a honeycomb lattice
B phase: Dirac Majorana fermions (Z2 QSL)

## Slide 39
Na2IrO3 & α-RuCl3 : 2D honeycomb lattice/edge sharing octahedra
F. Ye et al.,
PRB 85, 180403 (2012)
K. W. Plumb et al.,
PRB 90, 041112 (2014)
Na2IrO3 : Ir4+, 5d, s=1/2
TN=18.1K, zigzag order
<M>= 0.22 μB/Ir
α-RuCl3 : Ru3+, 4d, s=1/2
meff= 1.73μB; U = 1.5 eV

## Slide 40
RuCl3: SOC Mott Physics
Zigzag Magnetic ordering
H.-S. Kim et l.,
PRB 91, 241110 (2015)
Jackeli &Khaliullin
PRL 102, 017205 (2009)

## Slide 41
Kitaev spin liquid (KSL) or Proximate KSL behaviors?
Magnon
(gapped)
Continuum?
A. Banerjee et al., Nature Mater.15, 733(2016)
Gapped Spin excitations in Kitaev QSL:
2 Majorana Fermions + 1 Ising flux
G. Baskaran, et al, PRL 98, 247201 (2007).
K. Ran et al., PRL 118, 107203 (2017)

## Slide 42
field suppression of the AFM order
Hc ~7.5 T;
a very sharp 2nd or a 1st order transition
AB
stacking
ABC
stacking
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 43
35Cl NMR: 3 sites * (1 center + 2 satellites)* PM/AFM=9/18 lines
Large Knight shift
Narrow Center spectra ~ 100 KHz
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 44
Field-suppressed Magnetic ordering: A 2D QSL?
ABC stacking
JZ WQY et al.
PRL 119, 227208 (2017)
AB stacking
Johnson et al.,
PRB 92, 235119 (2015)
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 45
A field-induced Gapless quantum disordered phase
Nodal-like (gapless) excitations below 16 T
Gapped at H > 16 T
JZ WQY et al.
PRL 119, 227208 (2017)
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 46
(Bosonic) Paramagnetic
d-wave superconductor
(Fermionic) Nodal/Dirac-cone like excitations
 spin liquid?
 Dirac cones at specific angles by K,  model?
Z. Liu & Bruce Normand, PRL 120, 187201 (2018)
A novel quantum spin liquid?
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 47
Candidate mechanisms below 16 T
Spin excitations in ideal Kitaev spin liquid:
two Dirac Majorana Ferminons + a gapped flux gapped
(G. Baskaran, S. Mandal, and R. Shankar, PRL 98, 247201 (2007).
Spin excitations in Kitaev spin liquids under field
gapped Majorana Fermions +flux gapped
3. Spin excitations in 2D Heisenberg under field
magnetization plateaus or the fully saturated states  gapped
X
X
X
JZ WQY et al. PRL 119, 227208 (2017)

## Slide 48
Summary on α-RuCl3
1. A field-induced spin liquid is suggested at H>7.5 T//ab.
2. Gapless (partially gapped) excitations are observed above
the critical field.
3. Nodal-like excitations are suggested, which may be an
evidence of Dirac spinons for a spin liquid.
 Novel physics toward SOC Mott insulator

## Slide 49
iv. Proximate deconfined quantum critical point in a Shastry-Sutherland material
Y. Cui et al., arXiv:2204.08133 (to appear in Science)

## Slide 50
DQCP: Numerical proposals & properties
Continuous QPT
(Beyond the G-L paradigm)
Deconfined fractional excitations (Spinons) in the Quantum critical regime
Emergent symmetry: O(2)⊗Z(4)O(4)?
change of the Berry phase
High-Tc mechanism (SO(5))?
T. Senthil et al., Science 303, 1490 (2004);
R. R. P. Singh, Physics 3, 35 (2010);
Sandvik, PRL 104, 177201 (2010);
H. Shao et al., Science, 352, 213 (2016).
……
CBJQ model

## Slide 51
禁闭：磁有序和自旋波理论
玻色型元激发
S = ½ 三维铁磁体零温时的磁构型
非零温时的自旋波涨落 ：磁振子
单一色散关系

## Slide 52
2)解禁闭途径一：反铁磁海森堡自旋链（S = ½）
SrCuTe2O6，中子散射连续谱， S. Chillal et al., PRB 104, 144402 (2021)

## Slide 53
解禁闭：S = ½ 反铁磁海森堡自旋链中的自旋子
解禁闭的分数化元激发（S= ½，费米型）
一维S=1/2 反铁磁系统
vs
Quantum Magnetism, by Schollwöck et al.
连续谱

## Slide 54
解禁闭：自旋阻挫体系和量子自旋液体
量子自旋液体态 (S=0) & 解禁闭自旋子
三
角
晶
格
笼
目
晶
格
烧
绿
石
晶
格
蜂
巢
Kitaev
模
型
在-RuCl3 中，通过磁场调控发现具有无能隙自旋子的量子自旋液体态特征。 J. Zheng et al., PRL 119, 227208 (2017)

## Slide 55
DQCP in EPJQ model
Excitation continuum
Gapless at (π,0) & (π, π);
Spinon coupled to an emergent gauge field
N. Ma et al.,
PRB 98, 174421 (2018).
Regular QCP
No continuum
Artificial model: EPJQ and fractionalization
Notes: 对比 π0 和ππ位置都无能隙的连续谱；并且整个能谱的下边界，谱权重明暗分布有强烈的变化，这说明spinon不是不理的自由粒子，而是与分数化过程中的演生出来的规范场强烈耦合正。能谱中权重明暗的变化其实是物质场和演生规范场强烈耦合的结果。说明DQCP和高能物理学中夸克禁闭到去禁闭相变的共通性，是在凝聚态物理系统中重现了高能物理学现象。

## Slide 56
II. Shastry Sutherland model (SSM) , materials, and quantum phase transitions

## Slide 57
Dimer singlet
Plaquette singlet
Shastry & Sutherland, Physica 108B, 1069 (1981);
A. Koga et al., PRL 84, 4461 (2000);
P. Corboz et al., PRB 87, 115144 (2013);
J. Guo et al., PRL 124, 206602 (2020);
……
A realistic model: Shastry-Sutherland model
DQCP? (价键晶体态---反铁磁态)
J/J ' < 0.675, exact dimer singlet
J/J ' >0.765, AFM
Plaquette singlet (VBS):
Mirror symmetry breaking by dimers &double degeneracy

## Slide 58
SrCu2(BO3)2 : A Shastry-Sutherland material
J '∼85 K, α = 0.635
Tetragonal: a = 8.995 Å
c = 6.649 Å
H. Kageyama et al., Physica B 329, 1020 (2003)；
M. E. Zayed et al., Nat. Phys. 13, 962 (2017).
SrCu2(BO3)2
J/J ' tuned by pressure

## Slide 59
J. Guo et al., PRL 124, 206602 (2020).
Quantum phase transition in SrCu2(BO3)2
Notes: AFM相互作用，导致基态为二聚体态。

## Slide 60
NMR Results Preview: (P, H,T ) Phase diagram
Y. Cui et al., arXiv:2204.08133
Plaquette liquid phase
full-plaquette VBS phase
AFM ordered phase
A proximate DQCP between VBS-AFM
Notes: Before going to the details , I would like to fist present our experimental results. Under a constant pressure at 2.1 GPa,
We found a plaquette liquid phase at high temperature.
At low temperatures, a full-plaquette ground state is identidfied in contrast to the pure SS model.
We also found the magnetic field suppresses the PS phase and induces a AFM phase with a nearly continuous phase transition which supports
A deconfined quantum criticality with emergent O(3) symmetry. Now let me try to convince you.

## Slide 61
III. NMR evidence of a Valence-bond-solid (VBS) state and an AFM state in SrCu2(BO3)2

## Slide 62
H is 8 away from c-axis
4 inequivalent B sites
high-pressure 11B (I = 3/2) NMR on SrCu2(BO3)2
f ~ 11γ|Hext+Hhf|+mνQ
Hyperfine field
Quadrupole splitting
m = 0, ±1 for I=3/2
Y. Cui et al., arXiv:2204.08133
Center peak: uniform χ
Satellites:
local lattice structure
Notes: 11B is a nice nuclei, as it has spin- three halfs. As shown by the specretra measured in a paramagnetic phase, the 11B spectra contains both a center line and two groups of satellites. Each satellite group has four lines, because each unit cell contains four inequivalent B sites. Note that the resonance frequency of the center peak detects the uniform susceptibility, and the satellite detects local lattice structure through the coupling between the nuclear quadruple moment and the local electric field gradient. By this, both lattice structure and magnetism can be measured.
With this, we would think NMR is a very good probe to reach a combination of high-pressure, high-field and ultra low temperature spectroscopic study.

## Slide 63
1) Pressure-induced full-plaquette (FP) VBS state
Y. Cui et al., arXiv:2204.08133
Large increase of FWHM below 1.8 K
Local EFG effect
Inequivalent B sites
Structural twinning of the FP phase
Notes: To probe sensitively the local lattice structure, we measured the NMR satellites at a very low field of 0.2 T, so that the magnetic
Broadening of the spectra can be mostly ignored.
We measured the satellite spectra upon cooling, with the lowest temperature of 0.1 K. By this, we found that the linewidth of
Each satellite first increase upon cooling, which indicates lattice fluctuations. Below about 2 K, the linewidth suddenly increases and reaches a large constant value below 1 K. This clearly indicates a phase transition at about 2 K. The increase of the NMR linewidth should indicated the development of the inequivalent B sites which are affected by local EFG. In particular, we think that this is constant with an FP phase.

## Slide 64
Empty plaquette (EP) vs full plaquette (FP) phases
Pure SS model: EP phase + Double degeneracy
Satellite
line split or broadening
Satellite
line narrowing
Modified SS model: FP phase + Double degeneracy
Notes: Why is this? In fact, for the pure SS model, a pressure induced empty plaquette phase is proposed, where the plaquette singlet does not include the dimer bond.
By this, all the B sites resides outside the local plaquette, so that the line narrowing should be expected, which is in contradiction with our results.
On the other hand, the full plaquette phase, inequivalent B sites would be induced at the same position in different domains. It will give the satellite line split or broadening if the split cannot be resolve, because B can be either insides or outside of the local plaquette, considering double degeneracy of the states.
This is indeed the first spectral evidence for the FP phase.

## Slide 65
2) field induced AFM at 2.1 GPa
double-peak spectra at fields above 6.2 T
AFM order due to dipolar Hchf
Phases coexistence at 6.2-6.3 T
Weakly first-order quantum phase transition.
Notes: Now, if a higher magnetic field is applied, we found that the center NMR line splits with temperature, clearly indicates an AFM magnetic ordering
Which induces both a positive and a negative hyperfine field relative to the external field. At fiels above 8T, the transition is pretty much like a second order phase transition as shown by the frequency difference of the peaks as a function of temperature, which observes the change of the order parameter.
The transition field, measured at about 0.07 K, show the line splits at about 6.2 T; However, just at about 6.2 T, three peak feature is observed, which suggests the coexistenc of two phases, and therefore a weakly first-order quantum phase transition. Then the question is, how weak it is?

## Slide 66
Field-induced AFM: A weakly first-order QPT
double-peak spectra above 6.2 T
AFM order; (dipolar Hchf)
Phases coexistence at 6.2-6.3 T Weakly first-order phase transition.
Magnetic moments lie in the ab plane, easy-plane order
Mstaggered < 0.05 B
Mtotal/Ms < 0.025 B
Proximate DQCP?
Y. Cui et al., arXiv:2204.08133

## Slide 67
IV. NMR evidence of a field-induced proximate DQCP in SrCu2(BO3)2
Y. Cui et al., arXiv:2204.08133 (to appear in Science)

## Slide 68
1: TP and TN determined by 1/T1
TP: plaquette phase transition
TN: AFM phase transition
TP & TN: Peak positions in 1/T1(T)
Y. Cui et al., arXiv:2204.08133
Notes: In fact, the phase transitions can be precisely determined by the NMR spin-lattice relations rate 1/T1.
At 2.1 Gpa, the 1/T1 data are shown as a function of temperature shown : for the low field, there is a peaked feature in 1/T1 at a specfic temprature , which reveals the onset of the plaquette phase.
At high fields, also a peaked feature is clearly seen in 1/T1 , which reveals the AFM phase transition.
Also for a pressure of 2.4 Gpa. Both the plaqutte transition temperature and the AFM transition temperature can be determined. However, the plaquette in the this one is determined by a deviations of the power-scaling which I am not going to the details.

## Slide 69
Y. Cui et al., arXiv:2204.08133
(H,T) Phase diagram at P = 2.1 GPa
A weakly first-order quantum phase transition
J. Guo et al., PRL 124, 206602 (2020)
J. L. Jimenez et al., Nature 592, 370 (2021)
Notes: All the transition temperature can be plotted as a function of field, such as at 2.1 Gpa. This is exactly the phase diagram that I show before.
Interestingly, the transition temperature drops sharply from both sides and meets at about zero temperature.

## Slide 70
Scaling behaviors  duality
TP,N = Tb + aP,N |H − Hb|ϕ
2.1 GPa:
Hb = 6.184±0.05 T
Tb= 0.066±0.010 K
ϕ = 0.569±0.025
2.4 GPa:
Hb = 5.719±0.006 T
Tb= 0.062±0.012 K
ϕ = 0.498±0.031
2: A Proximate DQCP
Small Tb  a proximate DQCP;
Duality  an emergent symmetry to support the DQCP
Y. Cui et al., arXiv:2204.08133
Notes: In fact, our careful measurents show that for bout 2.1 Gpa and 2.4 Gpa. The PS and the AFM are connected by a bicritical point with a temperature about 0.06 K. This suggests that the transition is nearly continuously, which supports a proximate DQCP.
Furthermore, the transition lines are found to follow a power-law field dependence when away from the critical field; In fact the power-law exponent is identical for both the PS and the AFM phase, which suggests a duality of two phases. Therefore, an emergent symmetry is suggested to support the DQCP.

## Slide 71
Fits of the TP and TN: scaling and duality
TP,N = Tc + aP,N|H0 − Hc|φ
TP,N = AP,N ln−1 |CP,N(H − Hc)|
Y. Cui et al., arXiv:2204.08133

## Slide 72
3: Level crossing of the plaquette gap
CBJQ model, SSE+QMC
Gapless at the QPT
Close to a continuous transition
Emergent continuous symmetry?
1/T1T∼ e−∆/KBT in the PS state;
Δ decreases linearly with fields and vanishes at the QPT.
Y. Cui et al., arXiv:2204.08133

## Slide 73
4: Quantum criticality
1/T1= b(H) + aTη
bH ∞ (Hc − H0)d
η = 0.20±0.02;
d = 0.77±0.04
Y. Cui et al., arXiv:2204.08133
2.4 GPa vs 2.1 GPa data
Lower staggered m at Hc;
2.4 GPa is closer to the DQCP
Proximate DQCP

## Slide 74
5: Emergent Symmetries
In the PL phase
Double-peak
At the transition
Uniform distribution
In the AFM phase
Single-peak
Z2 symmetry breaking
U(1) symmetry breaking
mp: the order parameter of the PL phase
Emergent O(3) symmetry from U(1)*Z2
Y. Cui et al., arXiv:2204.08133
SSE+QMC on CBJQ Model
Notes: This is indeed supported by the numerical simulations based on CBJQ model.
The histogram of the plaqute order mp has a double peak at low field, but a rectangular type at the critical field, which suggest that there is an emergent O(3) symmetry, which recovers from the U(1) symmetry breaking in the AFM phase and the Z2 symmetry breaking in the plaquette phase.

## Slide 75
Future studies 1: (P, H, T) phase diagram
The first experimental realization of a proximate DQCP, which offers a platform for studies of novel properties.
O(4) DQCP at higher pressures?
Fractional excitations?
Multiple critical point?
QSL?
Notes: We further compare the data between 2.1 Gpa and 2.4 Gpa. It found that at the critical field, the staggered m is lower at higher pressures, which indicate the transition is more continuous; The smaller power-law exponent fai at 2.4 Gpa also suggests a more continuous transition at 2.4 GPa. Therefore, 2.4 Gpa is closer to the DQCP. This is illusteated by a 3D cartoon phase diagram with (P, H, T). With increase of pressure, the system going towards a real DQCP which connect to a possible QSL.

## Slide 76
2: Plaquette Liquid phase
Decrease of uniform χ
f1  DS phase
f2  PS phase
Phase coexistence at 1.85 GPa
Y. Cui et al., arXiv:2204.08133
Ahf <0

## Slide 77
P < 1.85 GPa, a crossover to the DS;
P  1.85 GPa, a sharp crossover at T* with no evidence of symmetry breaking plaquette liquid phase A QSL?
Y. Cui et al., arXiv:2204.08133
Ahf <0
Plaquette Liquid phase

## Slide 78
J. Guo et al., PRL 124, 206602 (2020)
first-order
J. L. Jimenez et al., Nature 592, 370 (2021)
Pressure homogeneity is very important!
3: homogeneous vs inhomogeneous P
Notes: SBCO is a SS materials which is tunable by pressure, and offers very interesting phases as illustrated by the phase diagram which were constructed by the previous speaker and also Jimenez at al. It contains dimerized singlet phases, Plauette singlet phase and antiferromagnetic phase with increasing pressures.
However, there are still outstanding questions. Because these phase diagram are constructerd by the specific heat,
Spectrascopic studies are needed to confirmed these phase, and also the structure of the phases. For example. Is the plaqutte phase of an empty plquett or a full plaqutte phase? Second, is there a continuous phase transition between the plaquette singlet and the AFMphase to support a dQCP? But this is a hard question, because 2.5 Gpa and avove is very hard to obtain. In this work, we would focus on the NMR study on two pressures slightly below 2.5 Gpa, that is, 2.1 and 2.4 GPa

## Slide 79
Summary
Symmetry breaking evidence for a pressure-induced full-plaquette VBS phase are established in SrCu2(BO3)2.
A pressure-induced plaquette liquid phase is observed.
Symmetry breaking evidence for a field-induced AFM phase are resolved in SrCu2(BO3)2.
A proximate DQCP is firmly established for the first time.
  Low transition temperature at the QPT
  Duality of TP and TN with field
  Quantum Critical scaling
  An emergent O(3) symmetry
Y. Cui et al., arXiv:2204.08133 (to appear in Science)
Notes: Finally, I would like to summarize our resluts. We resolved a full plaquette phase and the for the first time.
We also found a field-induced weakly first-order QPT between PS and the AFM phase.
A duality of TP and TN is also suggested by a power-law scaling behavior.
From this, we conclude that a primicate DQCP with emergent symmetry is established.
With this initiative work, studies are proposed. The first is to look for direct evidence of fractional excitations at the proximated DCP; the second is to study the phase as even higher pressures? Would there be a DQCP and QSL? Thank you for your attention.